MoS-2 MolybdenumDisulphide  solid lubricant dispersion in mineral oil. Ad to Gearoils / industial oils.

Solid lubricant dispersion in mineral oil for metal/metal combinations involving medium to high loads and speeds

Applications
Suitable for oil lubricated friction contacts requiring additional lubrication to reduce wear and to extend service life
Used successfully as an additive to oil, for example: on highly stressed plain and roller bearings, guides, spindles and gears, also in cutting and non cutting metalworking. It has also use in engines for protection against wear dry running. Use  in Compressors and hydraulic systems has also been done with success.

Temperature: service temperature °C depends on the lubricating oil used, so PAO  and  Esters will allow higher temperature than mineral oil.

For professional use only. The above information is given in good faith but without warranty and does not
constitute a technical specification. For technical support and application guidance call +45 70 26 70 07 or sq@reinhardoil.dk
Properties
Fluid Concentrate do mix well with all mineral oils and part synthetic as well as fully synthetic motoroils and industrial oils Group 2, 3 and 4., hydro cracked mineral oils and PAO synthetic fluids and many esters, but NOT PolyGlycol gear oils.

Fluid Concentrate is stable, also at higher permanent thermal and dynamic loads and can pass filters i most r normal filter systems without ending up all in the filter.

Fluid Concentrate  reduces run in and normal wear, improves the lubrication under high pressures,   and under normal working conditions, and provides some insurance against dry (shortly  running without serious damages. Lowing the friction can also give some reduction in oil and fuel consumption.

FC gives safe lubrication for longer equipment life /wear parts life  and protects against short dry running.

# Typical properties

Carrier			Neutral mineral oil ISO 100 (SAE 30) Solvent refined.

Colour			Gray-black to black

MoS2  specification       		MIL-L-7866 B, DEF 2304, CS 2819

MoS2  particle size   		0,5 my i average

Dry content MoS-2		5 %

Usefull Temperatures          	as mineral oils , they will carbonise at higher temperatures,

but gives dry lubrication shortly up to 400°C.

Useful area        	Ad to motor- gear- hydraulic- , Compressor- oand cutting oils,

where the demands ar high.

Use	Ad to lube oil/fluid  3 - 5 %. By extreme demands up to 10%, but then you have ot keep an eye at the filters to ensure full flow through the filters

MolyDane is a  program of special lubricants                               2010-01-03 SQ